Research Article

Available Online at: www.ijpir.com

# International Journal of Pharmacy and Industrial Research

ISSN	Print	2231 – 3648

Online	2231 – 3656

FORMULATION OF TRANSDERMAL PATCH BY FACTORIAL DESIGN IN MANAGEMENT OF HYPERTENSION: IN VITRO, EX VIVO AND IN VIVO SKIN IRRITATION EVALUATION

# *1Sunitha Sampathi, 2Sravanthi Anampally, 1Nataraj Narra.

*1 Department of Pharmaceutics, National Institute of Pharmaceutical Education and Research (NIPERH), Balanagar, Hyderabad, A.P. 500037, India.

2 Department of Pharmaceutics, Srikrupa Institute of Pharmaceutical Sciences, Vill: Velkatta, Siddipet. District: Medak, A.P. – 502103. India.

## Abstract

An attempt was made to formulate and evaluate the trandolapril transdermal drug delivery system. The matrix type films were prepared by 32 factorial design using solvent casting technique with polymers like Eudragit RL 100 and HPMC K15M. Di-butyl phthalate and DMSO were used as plasticizer and penetration enhancer. The prepared films were evaluated for physicochemical characteristics. The drug excepient Compatibility was determined by Fourier transform infrared spectroscopy and Differential scanning calorimetry. In vitro permeation studies were performed using Franz diffusion cell. Ex vivo studies were performed using skin of albino rats. The results revealed that there is no interaction between drug and selected polymers. Drug content varied from 96.43 ± 0.38 - 99.08 ± 0.8%. Moisture content and moisture uptake were increased for the patches containing higher amount of HPMC due to its hydrophilic nature. It was found that the formulation release followed first order release kinetics with non-fickian anomalous diffusion of drug release mechanism.

Key words: Trandolapril, Eudragit RL 100, HPMC, Transdermal matrix films

## Introduction

Tremendous efforts have been focussed on the development of new drug delivery systems [1]. Transdermal drug delivery system was introduced to overcome difficulties faced by the oral drug delivery systems. Transdermal patches are mainly used to deliver a specific dose of drug through the skin into blood stream and this was first approved by FDA in 1981. Transdermal delivery mainly provide sustained release of drug and useful for drugs with short half life [2].These also improves patient compliance and interruption or termination of treatment when necessary [3]. Trandolapril (TLP)

the esterified prodrug of the active metabolite trandolaprilate is a nonsulfhydryl angiotensin- converting enzyme (ACE) inhibitor. It is approved for the management of hypertension and for use in stable patients who have evidence of left ventricular systolic dysfunction or symptoms of chronic heart failure within the first two days after acute myocardial infarction. TLP undergoes extensive first-pass metabolism leading to poor bioavailability of 9.5% [4]. It is converted by esterases into the diacid metabolite, trandolaprilate (bioavailability 40-60%), which is approximately, eight times more active as an inhibitor of ACE

Address for Correspondence:

Sunitha Sampathi,

National Institute of Pharmaceutical Education and Research (NIPERH), Balanagar, Hyderabad, A.P. 500037, India.

Email ID: sunithasampathiphd@gmail.com

activity. Peak plasma concentrations (Cmax) of TLP were 1.68 to 1.88 ng/mL and were achieved with in

0.5 to 1.5 h when a single oral 2 mg of TLP was administered to healthy subjects [5, 6]. It possess ideal characteristics such as low molecular weight of 430.54, logarithmic partition coefficient in octanol/water is 1.28 [7], smaller dose (1-4 mg), short elimination half life (0.7 h), and poor oral bioavailability (9.5%) for formulation as transdermal patches. Polymers used should also precede consistent and effective delivery of the drug throughout the products intended shelf life and should be GRAS. Naturally occurring penetration enhancers like essential oils, terpenes, d-limonene, eucalyptus oil, peppermint oil, and turpentine oil are also clinically acceptable enhancers [8, 9]. In the present study DMSO was used as penetration enhancer and di-butyl phthalate as plasticizer. The objective of the present study is an attempt to develop and evaluate the TLP transdermal system for physicochemical characteristics, compatibility studies and for in vitro release and ex vivo permeation studies.

Materials and methods

## Materials

TLP was generous gift sample from Hetero Drugs Pvt. Ltd. (Hyderabad, India). Eudragit RL 100 was a gift sample from Natco, India, Hyderabad. Hydroxypropyl methylcellulose 15 cps, DMSO, disodium hydrogen phosphate, potassium dihydrogen phosphate, and sodium chloride were purchased from SD Fine Chemicals, Pvt. Ltd (Mumbai, India).

## Experimental method

Preparation of the Transdermal films

Matrix type patches loaded with TLP were prepared by solvent casting method. The transdermal films containing Eudragit RL 100 and HPMC with 2 mg of drug per patch size of 2.25 cm2 of TLP wt/wt with plasticizer (Dibutyl phthalate) and DMSO 5% as penetration enhancer were prepared. Hydrophilic ingredients were dissolved in distilled water and the hyphophobic ingredients were dissolved in ethanol and were then mixed and stirred on a cyclomixer to get homogenous mixture. The resulting solution was poured into a Teflon petridish of area 18.066 cm2 containing 16 mg of the drug. An inverted funnel was placed over the petridish to prevent the fast evaporation of the solvent after a period 24h the dried medicated transdermal film were placed in a plastic seal bag and stored in desiccators [11, 12].

## Factorial design

The formulation compositions are optimized by factorial design following 32 factorial analysis design. This experiment using factorial design allows one to examine simultaneously the effects of multiple independent variables and their degree of interaction. The formulae were developed as 9 sets varying the variables (polymers) following 32 full factorial design (3 levels) using Design expert®. (Table 1, 2, 3).

Table No. 01: Formulation and design of 32 full factorial experiment design layout

Trial	Variable level in coded formulation

|  | (X1) | (X2) |
| --- | --- | --- |
| 1 | -1 | -1 |
| 2 | -1 | 0 |
| 3 | -1 | +1 |
| 4 | 0 | -1 |
| 5 | 0 | 0 |
| 6 | 0 | +1 |
| 7 | +1 | -1 |
| 8 | +1 | 0 |
| 9 | +1 | +1 |

Table No. 02: Values of amounts of variables in 32 full factorial design

| Coded values | Actual values (X1=Eudragits RL100) | Actual values (X2 =HPMC- 15cps) |
| --- | --- | --- |
| -1 | 350 | 350 |
| 0 | 450 | 450 |
| +1 | 550 | 550 |

## Analytical method

Accurately 50 mg of drug was weighed and placed in a 50 mL volumetric flask and dissolved in phosphate buffer of pH 7.4 and volume adjusted to

50 mL. The Standard solution of drug was subsequently diluted with phosphate buffer to obtain a series of dilutions containing 5, 10, 15, and 20 µg/mL of the solutions. The absorbance of the

above dilutions was measured in double beam (Jasco) UV spectrophotometer at 224 nm with a quartz cell of 10 mm path length against phosphate buffer. A graph was plotted by taking concentration of TLP µg/mL on x-axis and absorbance on y-axis. The concentration of drug was calculated using the linear regression equation of the calibration curve.

Design Summary

Table No. 03: Factorial design (32) Summary with responses

| Study Type | Factorial |  | Runs | 9 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Initial Design | Full Factorial |  | Blocks | No Blocks |  |  |  |  |  |
| Center Points | 0 |  |  |  |  |  |  |  |  |
| Design Model | 2FI |  |  |  |  |  |  |  |  |
| Factor | Name | Units | Type | Low | High |  |  |  |  |
| A | Eudragit RL100 | mg | Cat | 350 | 550 | Levels: | 3 |  |  |
| B | HPMC K15 | mg | Cat | 350 | 550 | Levels: | 3 |  |  |
| Response | Name | Units | Obs | Analysis | Min | Max | Mean | Std. Dv. | Ratio |
| Y1 | Q 24 | % | 9 | Factorial | 44.33 | 73.6 | 55.076 | 9.2442 | 1.660 |
| Y2 | Q 8 | % | 9 | Factorial | 15.5 | 38.43 | 27.735 | 6.9483 | 2.479 |
| Y3 | RRC 1st Order |  | 9 | Factorial | 0.0104 | 0.023 | 0.0146 | 0.0039 | 2.211 |

## Evaluation of physicochemical properties of the patches

Thickness and Weight variation

The thickness of the patches was checked at six different points of the film using a micrometer. For weight variation three films each of 1 cm2 from each batch were weighted individually and the average weight was calculated.

## Folding Endurance

The folding endurance was measured manually as per the method reported [10]. A strip of the film was cut and repeatedly folded at the same place until the film breaks. The more thin the film the more will be the flexibility of the film.

Other mechanical properties like tensile strength (TS), elastic modulus (EM) and elongation at break (E/B) were evaluated by using tensile strength apparatus (Ultra Test, Mecmesin, UK) equipped with 25 kg load cell. Film strip with dimensions 60mmX10mm and free from air bubbles or physical imperfections were held between two clamps positioned at a distance of 3 cm. during measurement, the top clamp at a rate of 2 mm/s pulled the strips to a distance till the film broke. The force and elongation were measured when the film broke. The mechanical properties were calculated according to the below formulae [14]. These properties were evaluated to confirm the physical quality of the patch which denotes patch/film durability and physical stability.

Mechanical properties

# Tensile strength (kg. mm-2 ) 

Force at break (kg)

# Initial cross sectional area of the sample (mm2 )

Elongation at break (% mm-2 )  Increase in length (mm) X

Original length (mm)

100

Cross sectional area

# Elastic modulus  Force at corresponding strain (kg) X

Cross sectional area (mm2 )

# Strain  Tensile strength

Elastic modulus

100

# Corresponding strain

## Drug content

The drug content was determined by taking a patch (2.25 cm2) cut it into small pieces and added to a beaker containing 100 mL of PBS (pH 7.4). The film was completely dissolved by cyclomixer. The contents were filtered using Whattman filter paper and the drug content in the filtrate was estimated using a UV spectrophotometer at 244 nm using the reference solution consisting of placebo film.

Percentage of Moisture Content

The dried films were weighed individually and kept in a desiccator containing activated silica. The films were weighed regularly until a constant

weight was obtained. The percentage of moisture content was calculated as the difference between initial and final weight with respect to the final weight [17].

Percentage of Moisture Uptake

The dried films were weighed and placed in desiccators containing 200 mL of saturated solution of potassium chloride (84% relative humidity) at room temperature. The percentage moisture uptake of the films was calculated as the difference between final and initial weight with respect to the initial weight [15].

Skin irritation test

% Moisture Uptake  Final Weight  Initial Weight X100

Initial Weight

prepared transdermal film of 2.25 cm2 was placed

The test was performed on a healthy albino rat weighing around 175 g. Aqueous solution of formalin 0.8% was used as the standard irritant. Placebo polymer patch of 2.25 cm2 were used as the test patch. Standard irritant was applied on the left dorsal surface of each rat and placebo patch was applied on the right dorsal surface of the albino rat [Ethical Committee Reg. No: 1548/PO/a/11/CPCSEA]. The patches were removed after period of 24 h with the help of an

alcohol swab. The skin was examined for erythema or edema [2, 13, 16].

## Drug-polymer compatibility studies

Fourier Transforms Infrared Spectroscopy (FTIR) and Differential scanning calorimetry (DSC) were used to know the compatibility between the drug and polymers used in the patches, by KBr pellet method in the wavelength region between 4000 to 400 cm-1 the FTIR and DSC was performed for the pure drug, polymers and the physical mixtures of drug and the polymers used and were compared.

In vitro drug release studies

In vitro drug release studies were performed by using a Franz diffusion apparatus. The dialysis membrane was mounted between the donor and receptor compartment of the diffusion cell [18]. The

on the membrane which was previously soaked in phosphate buffer. The receptor compartment was filled with PBS pH 7.4. The total assembly was placed on a hot plate magnetic stirrer and stirred by maintaining the temperature at 32 ± 0.5°C. 5 mL of the samples were withdrawn at regular interval and replaced with an equal volume of PBS. The drug content was estimated spectrophotometrically at 244 nm.

Ex vivo skin permeation studies

The studies were performed by taking the rat skin as the membrane. Young albino rats weighing between 200 g to 250 g were taken and scarified by excess of chloroform inhalation. The abdominal hairs were removed and the abdominal skin was carefully separated from the body with the dermis part remaining intact. Subcutaneous tissue was surgically removed. The inner part of the skin was washed with distilled water thoroughly to separate the adhering fat. The full thickness of skin obtained was placed in normal saline solution and stored at 4

± 1°C until used for the experiment. The drug permeation from the transdermal patch through the skin was determined using Franz diffusion cell where the contents of donor and receptor was separated by placing the excised skin and the transdermal patch of 2.25 cm2 containing the drug

was placed in the donor compartment containing the stratum corneum side of the skin. The Franz diffusion cell was placed on a magnetic stirrer and stirred by placing Teflon coated bead at 500 rpm. Samples were withdrawn periodically and replaced with PBS to maintain skin condition. The drug content was estimated spectrophotometrically at a wave length of 244 nm.

## Results

Trandolapril transdermal patches were prepared and evaluated for various physical and release parameters. FTIR and DSC studies results revealed the drug excepient compatibility In IR spectra of trandolapril pure drug many number of peaks were found prominently at various wave numbers indicating the presence of functional groups & substitutions like peaks at 1650cm-1, wave number

due to C-C stretching in aliphatic chain, prominent peaks at 1736cm-1, 1280cm-1, 1458 cm-1 and 1193 cm-1 due to C=O stretching, C-O stretching, C-O-H stretching, and C-O-C stretching in aliphatic chain respectively indicating presence of carboxylic group and keto group in the structure. Broad peaks appeared between 3448 cm-1, 2943cm-1 wave number are due to C=C stretching in aromatic structure. Peaks appeared at 3270cm-1 and 1366cm-

1 were because of C-H stretching aromatic and definite in CH2 aliphatic respectively. A more intense peak was found at 3280cm-1 because of N- H stretching indicating presence of amino group in the structure & peak at 1433cm-1 wave number also indicates the presence of C-N stretching. All these peaks were appeared unchanged in IR spectra of combinations like trandolapril + EU + HPMC. (Figure 4).

| Table No. 04: Physical properties of prepared trandolapril transdermal patches |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Formulation | Weight | Thickness | Folding | Drug content | Moisture | Moisture |
| code | (mg/2.25 cm2) | (mm) | Endurance | (%) | uptake | content |
| TF1 | 57.14±0.96 | 1.16±0.06 | 137±3.60 | 99.08±0.8 | 8.57±0.59 | 4.39±0.46 |
| TF2 | 54.41±1.02 | 1.13±0.05 | 165±5.68 | 97.54±1.09 | 16.80±2.55 | 2.72±0.50 |
| TF3 | 46.4±1.8 | 1.01±0.05 | 222±3.21 | 97.85±0.91 | 18.92±0.34 | 4.55±0.38 |
| TF4 | 45.40±1.04 | 0.99±0.05 | 142±7.09 | 97.33±0.77 | 9.98±0.30 | 2.12±0.30 |
| TF5 | 61.55±1.37 | 0.96±0.18 | 124±8.71 | 98.10±0.84 | 18.36±0.95 | 2.4±0.24 |
| TF6 | 57.64±1.17 | 0.96±0.04 | 175±6.80 | 97.52±0.55 | 15.69±0.38 | 4.25±0.18 |
| TF7 | 58.11±30.62 | 1.03±0.05 | 129±7.23 | 98.73±0.36 | 15.22±0.75 | 3.41±0.22 |
| TF8 | 52.67±1.11 | 1.02±0.04 | 132±3.78 | 96.43±0.38 | 17.94±0.53 | 1.24±0.21 |
| TF9 | 41.86±0.79 | 1.03±0.044 | 135±4.04 | 97.54±0.55 | 17.48±0.66 | 2.62±0.23 |
| Table No. 05: Release kinetic data of transdermal patches formulations (TF1-TF9) |  |  |  |  |  |  |

| Formulation | Zero Order | First Order | Higuchi | Peppas |  |
| --- | --- | --- | --- | --- | --- |
|  | (R2) | (R2) | (R2) | n | (R2) |
| TF1 | 0.9185 | 0.9723 | 0.8409 | 0.5341 | 0.9133 |
| TF2 | 0.9242 | 0.9744 | 0.9807 | 0.6557 | 0.9887 |
| TF3 | 0.990 | 0.9815 | 0.982 | 0.6329 | 0.988 |
| TF4 | 0.9666 | 0.9924 | 0.9579 | 0.6215 | 0.9849 |
| TF5 | 0.9607 | 0.992 | 0.9608 | 0.5791 | 0.9842 |
| TF6 | 0.9451 | 0.9917 | 0.9753 | 0.5875 | 0.9815 |
| TF7 | 0.8662 | 0.9286 | 0.943 | 0.7814 | 0.9856 |
| TF8 | 0.9677 | 0.9977 | 0.9498 | 0.6363 | 0.9723 |
| TF9 | 0.973 | 0.9967 | 0.9515 | 0.7474 | 0.9878 |

The melting point of pure trandolapril was found at 127.91oC & followed exothermic type of reaction where onset was started 123.26oC & ends with 131.21oC (Figure 3). The glass transition lag was found around 7.95oC & the same exothermic type of reactions was found in all combinations like trandolapril + EU + HPMC. No change was found

in melting point as well as glass transition lag but special peaks were found indicating melting point of eudragit at 98.22oC, HPMC at 110.21oC, & the influence of excepients were found only in changing on’s & end’s sets of melting point peaks of drug by absorbing heat but not by interactions. Finally, DSC  data states that the crystallinity of

pure drug found unchanged & stable, and indirectly	determines the compositions are compatible.

Cumulative % drug release plots of trandolapril transdermal patches (TF1-TF9)

80

70

60

50

40

30

20

10

0

0

5

10

15

Time (h)

20

25

30

TF1

TF2

TF3

TF4

TF5 TF6 TF7

TF8

TF9

% Drug release

Fig. 01: In vitro drug release plots of formulations TF1 – TF9

70

Ex vivo skin permeation studies plot of best release formulation in vitro (TF2)

60

50

40

30

20

10

0

0

5

10

Time (h)

15

20

25

30

TF2

% Drug release

Fig. 02: Ex vivo drug skin permeation studies plot of formulation TF2

Average weight of the patch with an area of 2.25 cm2 was found least in formulation TF9 around

41.86 ± 0.79 and highest in TF5 61.55 ± 1.37 mg. Thickness was found more in formulation TF1 1.16

± 0.06 and less in TF6 0.96 ± 0.04 mm. Folding endurance was found to be more with TF3 formulation 222 ± 3.21 and less in TF5 124 ± 8.71,

% Drug content was found highest in TF1 99.08 ± 0.8% and least in TF8 around 96.43 ± 0.38. Moisture uptake and moisture content was found more in TF1 and TF3 around 18.92 ± 0.34% and

4.55 ± 0.38% respectively and less in TF3 and TF8

around 8.57 ± 0.59% and 1.24 ± 0.21% respectively. Highest values of tensile strength and elastic modulus was found to be in formulation TF1 around 1.93 ± 0.156 kg/m2 and 3.66 ± 0.335 kg/mm2 respectively with strain value of 0.527 and least values of above were found in formulations TF7 and TF5 around 0.96 ± 0.51 kg/m2 and 0.56 ±

0.115 kg/mm2 respectively. Elongation at break was found more in TF2 around 161.3 ± 2.46 and less in formulation TF7 around 74.5 ± 4.016 (Table 4).

Fig. 03: DSC overlay thermograms of pure drug trandolapril, polymer blend and drug with polymer.

Fig. 04: FTIR overlay spectra of trandolapril pure drug, polymers and pure drug with polymers

Design-Expert® Softw are

StdErr of Design

550.00

StdErr of Design Design Points 1.5

0.747

0.747

0.5

500.00

0.647

X1 = A: Eudragit RL 100 X2 = B: HPMC K15M

0.647

450.00

0.697

400.00

0.647

0.747

0.797

0.647

0.697

0.747

0.797

350.00

350.00

400.00

450.00	500.00

550.00

A: Eudragit RL 100

B: HPMC K15M

Fig. 05: Standard error of design counter plot of 32 full factorial design

Design-Expert® Softw are

StdErr of Design 1.5

0.5

1.000

X1 = A: Eudragit RL 100

X2 = B: HPMC K15M

0.750

0.500

0.250

0.000

550.00

550.00

500.00	500.00

450.00	450.00

B: HPMC K15M 400.00	400.00A: Eudragit RL 100

350.00     350.00

StdErr of Design

Fig. 06: Standard error of design 3D plot of 32 full factorial design

Design-Expert® Softw are

Q 24

73.6

44.33

X1 = A: Eudragit RL 100 X2 = B: HPMC K15M

74

66.5

59

51.5

44

550.00

550.00

500.00

500.00

450.00

450.00

B: HPMC K15M400.00

400.A00: Eudragit RL 100

350.00   350.00

Q 24

Fig. 07: 3D plot of Q24 % drug release influenced by HPMC and Eudragit combinations

Design-Expert® Softw are

Q 8

38.43

15.5

X1 = A: Eudragit RL 100 X2 = B: HPMC K15M

39

33

27

21

15

550.00

550

500.00	500

450.00	450

B: HPMC K15M 400.00	400  A: Eudragit RL 100

350.00     350

Q 8

Fig. 08: 3D plot of Q8 % drug release influenced by HPMC and Eudragit combinations

Design-Expert® Softw are

RRC 1st Order 0.023

0.0104

0.023

X1 = A: Eudragit RL 100 X2 = B: HPMC K15M

0.01975

0.0165

0.01325

0.01

550.00

500.00

550.00

450.00

500.00

B: HPMC K15M

450.00

400.00

400.00

350.00    350.00

A: Eudragit RL 100

RRC 1st Order

Fig. 09: 3D plot of release rate constant (first order) influenced by HPMC and Eudragit combinations

Fig. 10: Picture depicting the skin irritation test in rat by the formulation TF4

Fig. 11: Picture depicting the skin irritation test in rat by the standard (phenolic compound)

In In vitro drug release studies the more release retardation was found around 44.33 ± 2% in formulation TF4 up to 24 h where as less retardation was observed around 73.60 ± 2.1% in formulation TF5 after 24 h. All formulations followed first order non fickian release kinetics with anomalous transport mechanism (Figure 1) (Table 5, 6). Ex vivo characterization studies

carried by selecting formulation as per in vitro drug release results, with an intention to develop 48 h release plots formulation TF2 was selected to perform Ex vivo permeation studies (Figure 2). Release was found more as compared to in vitro results where 65.15±1.5% was release with in 24 h. Skin irritation test in rats proved that the formulations are found to be less irritant as

compared to standard with less erythema (Figure 10, 11). The in vitro data is used to calculate various other dependable responses like Q24, Q8 and first order release rate constant. The data was

plotted as surface response graph and analysed statistically where the p – value was found significant (less that 0.050) (Figure 4, 5, 6, 7, 8).

Table No. 06: Release of drug at 24 h, 8 h and release rate constant (first order)

| Formulation | Q24 (%) | Q8 (%) | Release rate constant (Ko) (first order) |
| --- | --- | --- | --- |
| TF1 | 46.89 | 15.50 | 0.0106 |
| TF2 | 48.37 | 25.33 | 0.0119 |
| TF3 | 58.33 | 32.27 | 0.0158 |
| TF4 | 44.33 | 21.50 | 0.0104 |
| TF5 | 73.60 | 34.53 | 0.0230 |
| TF6 | 56.87 | 29.33 | 0.0149 |
| TF7 | 55.50 | 38.43 | 0.0154 |
| TF8 | 65.47 | 31.50 | 0.0189 |
| TF9 | 46.33 | 21.23 | 0.0112 |

## Discussion

All physical parameters evaluation results were found in acceptable range. Folding endurance was found more with formulations with high percentage of eudragit than HPMC. Tensile strength was found more in formulations with high percentage of eudragit where as the elongation and elastic modulus were found more in formulations containing high percentage of HPMC than Eudragit. The drug release from the formulations was sustained over an extended period of time i.e. up to 48 h. The study states the release depended on the polymers ratio. Formulations prepared using HPMC showed better sustained action and formulation TF4 is confirmed as best formulation as it released maximum drug upto 48 h.

## Conclusion

The development of the 48 h releasing transdermal films by solvent casting could be adaptable in laboratory as well as in industry since it is simple and reproducible. In conclusion, HPMC and EU formulations could be used for better sustained action. However further in vivo studies are needed to optimize for sustained action in human beings for better bioavailability, efficacy thus safety.

## References

- Front line Strategic Consulting Inc. Alternative drug delivery systems series: Transdermal drug delivery systems, 2002, Front Line Strategic Consulting., Inc.

- Robinson JR, Lee VH. Controlled Drug Delivery: Fundamental and Applications; 2nd ed.; Marcel Dekker: New York, 1987; 523- 552.

- Guay DRP. Trandolapril: A newer angiotensin converting enzyme inhibitor. Clin Ther. 25(3), 2005, 713-775.

- Wiseman LR, Tanvish MC. Trandolapril: A review of its pharmacodynamic and pharmacokinetic properties, and therapeutic use in essential hypertension. Drugs. 48(1), 1994, 71-90.

- Danielson B, Querin S, LaRochelle P, Sultan E, Mouren M, Bryce T, Stepniewski J P, Lenfant B. Pharmacokinetic and pharmacodynamics of trandolapril after repeated administration of 2mg to patients with chronic renal failure and healthy control subjects. J Cardiovasc Pharmacol. 23, 1994, 50-59.

- Lenfant B, Mowren M, Bryce T, De Lauture D, Strauch G. Trandolapril: Pharmacokinetics of single oral doses in healthy male volunteers. J Cardiovasc Pharmacol. 23(4), 1994, 38-43.

- Remko M. Acidity, lipohilicity, solubility, absorption, and polar surface area of some ACE inhibitors. Chem Pap. 61(2), 2007, 133- 141.

- Williams A, Barry B. Terpenes and the lipid- protein partitioning theory of skin penetration enhancement. Pharm Res. 8(1), 1991, 17-24.

- Obata OH, Takayama K, Nagai T. Percutaneous absorption enhancing effect and skin irritation of monocyclic monoterpenes. Drug Disco Deliv. 6(3), 1990, 229-238.

- Das MK, Bhattacharya A, Ghosal SK. Transdermal delivery of trazodone hydrochloride from acrylic films prepared from aqueous latex. Indian J Pharm Sci. 68(1), 2006, 41-46.

- Deo MR, Sant VP, Parekh SR, Khopade AJ, Bankar UV. Proliposome based Transdermal delivery of levonorgesterol. J Biomat Appl. 12(1), 1997, 77-88.

- Rao PR, Ramakrishna S, Diwan PV. Drug release kinetics from polymeric films containing propanolol hydrochloride for transdermal use. Pharm Dev Technology. 5(4), 2000, 465-472.

- Wade Hull MS. Heat enhanced transdermal drug delivery: A Survey. Paer J Appl Res. 2, 2002, 1-9.

- Gannu R, Vishnu VY, Kishan V, Rao YM. Development of nitrendipine transdermal patches: In vitro and Ex vivo characterization. Curr Drug Del. 4, 2007, 69-76.

- Kusum Devi V, Saisivum S, Maria GR, Deepti PU. Design and evaluation of matrix diffusion controlled transdermal patches of verapamil hydrochloride. Drug Dev Ind Pharm. 29(5), 2003, 495-503.

- Libermmann and Lachman Pharmaceutical Dosage forms 2nd ed. Lea and Febiger; 1990: 265.

- Gupta R, Mukherjee B. Development and in vitro evaluation of diltiazem hydrochloride transdermal patches based on povidone- ethylcellulose matrices. Drug Dev Ind Pharm. 29(1), 2003, 1-7.

- Shinde AJ, Garala KL , More HN. Development and characterization of transdermal therapeutics systems of tramadol hydrochloride. Asian J Pharm. 2(4), 2008, 265-69.